1/8” Nitinol with no Oxide Coating

### Summary

Sphere Specs:

Manufacturer: Nitinol Technologies, Inc.

| Size | Material | Grade | Gage | Actual |
| --- | --- | --- | --- | --- |
| .125 in. | Nitinol |  |  |  |
| Lot No. | Qty | Code | Scan # |

Experiment Dates: Fall 2001 and 3/3-3/5/2002

Labview Time Delay: 10.00

Strobe: 12000 fpm

Scale for tracking program: 161 pixels/cm

Last fall and this spring, experiments were run on different types of Nitinol spheres. One was the original Natinol spheres, one was with black oxide coating, and one with the coating removed by a special grounding procedure. With respect to the original batch of Natinol spheres without any oxide coating, the binary collision experiments were run last fall and a set of results were obtained. We reduced the data again using the pictures from the last set of experiments and put it through the tracking program again, and we found that the new set of results varied quite significantly from the old set of results from last fall. Furthermore, it produced a number of data points with large and negative ψ1s and β0s.

The difference in results may have been due a different set of conditions which we used in the tracking program, as well as the value for pi used in the excel spreadsheet calculations. Based on latest measurements, we use a value of 161 pixels/inch in the tracking program. We also entered π as a function (i.e. “pi()”) which would use the full value of π in the calculation in the Excel spreadsheet, while we previously did not consistently use the same value of pi. However, the deviation in the two different sets of results still seem quite large for the changes that we made.

We examined the pictures from last fall again, and discovered that some of the later pictures (picture 41 and onwards) were inverted. In the earlier pictures, the top sphere was moving faster than the lower one, and after the collision, it would be slowed down, while the lower one would speed up. (This can be seen in the distance between the top and bottom spheres before and after the collision). In the pictures after no. 41, the trend was reversed – i.e. the top sphere was moving slower before the collision and speeded up after the collision. This would seem to indicate that the collisions had gone past head-on collisions. We tried taking out the pictures after complete head-on and reduced the data again. The results we obtained seemed to be more reasonable.

Set of Results from Fall

| e | (o | ( |
| --- | --- | --- |
| 0.98+/-0.02 | 0.60 +/- 0.13 | 0.13 +/-0.02 |

Initial Set of results with the rereduced data

| e | (o | ( |
| --- | --- | --- |
| 0.84 +/-0.08 | 1.98 +/- 3.31 | 0.11 +/-0.01 |

Set of results with the rereduced data with the later pictures removed

| e | (o | ( |
| --- | --- | --- |
| 0.95 +/-0.01 | 0.45 +/- 0.13 | 0.11 +/-0.01 |

#### Images

| Extreme grazing Picture No: 01 | Grazing Picture No: 12 |
| --- | --- |
| Collision Picture No: 29 | Head-on collision Picture No: 38 |

##### Results

For Fall ’01 Nitinol no oxide

“Binary Nitinol no Oxide2 Results.xls”

Rereduced data from Fall ’01 Nitinol no oxide

“Nitinol_NUO_ results2.xls”

Rereduced data with past head-on collisions taken out

“Nitinol Nox 2 results.xls”