3mm Titanium against 300 Series Stainless Bump

### Summary

Sphere Specs:

Manufacturer: Thomson Precision Ball Company, LLC

| Size | Material | Grade | Gage | Actual |
| --- | --- | --- | --- | --- |
| 3 mm | Titanium | 200 | OK | +0.000380 |
| Lot No. | Qty | Code | Scan # |
| 100447988 | 20 Pcs | 12B | TI0118112CXXXMM |

Experiment Dates: 4/15/02 – 4/18/02

Labview Time Delay: 10.00

Strobe: 12000 fpm

Scale for tracking program: 161 pixels/cm

To continue with our experiments involving Titanium spheres, following our binary collision experiments of Titanium vs Titanium and Titanium vs ceramic spheres, we ran experiments of Titanium spheres colliding against a 300 Series stainless bump. The initial setting up of the bump experiment proved to be quite time consuming, as the setup was significantly different from the binary experiment. We had to ensure that the clamp used to clamp the bump at an angle was accurately positioned below the drop tower, and also that when we adjusted the position of the sphere, it could capture the entire range from grazing to head-on collisions on the bump.

Another of the problems we encountered setting up the experiment was to make sure that the camera was aligned as accurately as possible along the axis of the bump. We had to do this a number of times, using the measurement and automation function of the camera software to ensure that the camera was properly aligned and that no shadows were visible in the picture. We had to rerun the experiment a number of times because we suspected from the pictures we were getting that the camera was not exactly aligned with the axis of the bump.

One more problem we had with bump experiments was that the direction the sphere would travel was highly unpredictable and changed considerably as we moved from head-on to grazing collisions, unlike binary experiments when the spheres would land close to directly below its falling axis. For bump collisions, the spheres would bounce off the bump in varying directions and we had trouble locating the spheres after some of the runs, taking a considerable amount of time in the process.

Once the setup was completed and we cleaned up the table, the experiment proceeded relatively smoothly and quickly. We were able to get a good range of pictures from head-on to grazing, and ended up with a total of 50 pictures. We put the pictures through Pete’s program and ran the data reduction spreadsheets with π as a function (i.e. “pi()” in Excel.

Results

| e | (o | ( |
| --- | --- | --- |
| 0.700 +/- | 1.43+/- 0.21 | 0.162 +/-0.005 |

The effective e we obtained, e’ where e’ = e – (π/2)*(, for Titanium was about 0.44.  Ideally for our experiments, we’d prefer e’ > 0.7, hence it would appear that Titanium is not that suitable for our purposes.

#### Images

| Head-on collision Picture No: 03 | Less Head-on Picture No: 12 |
| --- | --- |
| Collision Picture No: 32 | Grazing Picture No: 50 |

##### Results

“Ti Bump Results.xls”

(negative ()